## Slide 1: Head loss and velocity profiles Martine RUEFF FP1005 Cost Meeting 13-14 October 2011
Laboratoire de génie des procédés papetiers
Grenoble INP - Pagora
www.pagora.grenoble-inp.fr

## Slide 2: Objectives
To characterise pulp suspension flows at a low concentration (consistency below 4 %)
Head loss in straight pipes
Head loss in singularities
and to have a better insight of the suspension

## Slide 3: Who
MSc students: Ph. Dietemann (2003), L. Salgueiro (2004)
PhD students: J.D. Bonfanti (1997), L. Salgueiro (2008)
Interns
Supervised by Martine Rueff Jean-Claude Roux

## Slide 4: Test rigs
transparent pipes 120 / 80 / 50 mm
connections with smaller pipes, 17 to 40 mm, circular and rectangular cross- sections
max. flow rate 180 m3/h, 2 m3 storage tank
transparent pipe 65 mm
max. flow rate 120 m3/h,
1 m3 storage tank

## Slide 5: Test rigs
Hydraulic headbox, width 50 cm, with transparent parts jet velocity up to 30 m/s 15 m3 tank

## Slide 6: Equipment - sensors
Magnetic flow meters
Mass flow meter
Pressure sensors
Differential pressure sensors
Temperature sensors
Pulsed ultrasound Doppler velocimeter
High speed video camera / camcorder

## Slide 7: Type of pulps
Almost any pulp received in bales or liquid form stock preparation facilities waste return to the paper machine
Focus on chemical pulps

## Slide 8: Fibre suspension behaviour
100
80
60
40
20
10
80
60
40
20
10
80
mm
1 2 3 4 5 10 20 40 50 100 m3/h
DP/L , mbar/m
0.2 0.3 0.5 0.8 1.2 2.0 3.0 5.0 m/s
5.0 %
4.5 %
4.0 %
3.5 %
3.0 %
2.5 %
2.0 %
1.5 %
Water

## Slide 9: Pulsed Ultrasonic Doppler Velocimetry

## Slide 10: Pulsed Ultrasonic Doppler Velocimetry
Parameters
fe : transducer (size of particles)
q : transducer angle
Tprf : time interval between two pulses
Filter coefficients
Other factors
Refractive index of pipe wall

## Slide 11: Pulsed Ultrasonic Doppler Velocimetry

## Slide 12: Pulp suspension and experimental conditions
Bleached softwood pulp (maritime pine + traces of fir)
34 °SR
Length-weighted average length: 0.69 mm
Fibre coarseness: 0.226 mg/m
Consistencies: 0.47 %, 1.0 % and 2.1 %
Velocities : up to 7 m/s

## Slide 13: Experimental loop
Electromagnetic flow meter : 0-180 m3/h
Differential pressure sensor : 0-50 mbar

## Slide 14: Pressure drop curves

## Slide 15: Analysis of the velocity profiles

## Slide 16: Velocity profiles at 2.6 m/s

## Slide 17: Velocity profiles for 2.1 % consistency

## Slide 18: Volume fraction of “fluidised” suspension
Distance to centreline
Velocity
r
p
R

## Slide 19: Volume fraction of “fluidised” suspension

## Slide 20: Video images
Consistency, % 0.47 1.0 2.1
Beginning of “fluidisation”, m/s 0.2-0.7 1.4-2.8 1.4-2.8
Limit velocity for large aggregates, m/s 0.2-0.7 1.4-2.8 2.8
Apparition of relative motion, m/s / 2.1-4.1 4.1

## Slide 21: Conclusion
PUDV: non intrusive technique
Enabled us to explore a wide range of velocities and consistencies
From the velocities profiles, determination of:
  plug size
  volume fraction of fluidised suspension
  disruptive shear stress using pressure loss measurements

## Slide 22: Conclusion
The suspension was not totally homogeneous when drag reduction occurred
Video sequences showed the presence of large aggregates near the wall at relatively high velocities.